| COMPETENCY-BASED CURRICULUM |  |
| --- | --- |

| Sector: METALS AND ENGINEERING |
| --- |
| Qualification: Gas Metal Arc Welding (GMAW) NC III |
|  | Technical Education and Skills Development Authority East Service Road, South Superhighway, Taguig City, Metro Manila |

TABLE OF CONTENTS

Page

A. Course Design	1-5

B. Modules of Instruction	6-96

  - BASIC COMPETENCIES

  - Leading workplace communication	7-10

  - Leading small team	11-15

  - Developing and practicing negotiation skills	16-18

  - Identifying/ determining fundamental cause of problem	19-22

  - Using mathematical concepts and techniques	23-26

  - Using relevant technologies	27-30

  - COMMON COMPETENCIES

  - Applying safety practices	32-37

  - Interpreting drawing and sketches	38-41

  - Performing industry calculation	42-46

  - Contributing to quality system	47-50

  - Using hand tools	51-54

  - Preparing weld materials	55-60

  - Setting-up welding equipment	61-64

  - Fitting-up materials	65-67

  - Repairing weld	68-72

  - CORE COMPETENCIES

  - Performing groove welding on alloy steel plate.	74-80

  - Performing fillet welding on alloy steel plate	81-89

  - Performing groove welding on alloy steel pipe	90-96

# COURSE DESIGN

# COURSE TITLE	:	GAS METAL ARC WELDING (GMAW) NC III

NOMINAL DURATION	:	148 hours

COURSE DESCRIPTION	:

This course is designed to enhance the knowledge, desirable attitudes and skills of a WELDER in accordance with industry standards. It covers core competencies such as; weld alloy steel plates and weld alloy steel pipe using GMAW. This includes common competencies; apply safety practices, interpret drawing and sketches, perform industry calculations, contribute to quality system, use hand tools, prepare weld materials, setup welding equipment, fit up weld materials and repair welds. It also includes competencies such as, lead workplace communication, lead small teams, develop and practice negotiation skills, solve workplace problem related to work activity, solve mathematical concept and techniques and use relevant technologies.

ENTRY REQUIREMENTS	:

Candidate /trainee must posses any of the following qualifications;

- completed training in SMAW NC III and NC IV or a holder of GMAW NC II

- can communicate either orally and in written form

- physically  and mentally fit

- can perform basic mathematical computation

COURSE STRUCTURE:

# BASIC COMPETENCIES

(20 hours)

| UNIT OF COMPETENCY | MODULE TITLE | LEARNING OUTCOMES | NOMINAL DURATION |
| --- | --- | --- | --- |
| 1. Lead workplace communication | 1.1 Leading workplace communication | 1.1.1 Communicate information about workplace processes. 1.1.2 Lead workplace discussions. 1.1.3 Identify and communicate issues arising in the workplace. | 3 hours |
| 2. Lead small team | 2.1 Leading small team | 2.1.1 Provide team leadership. 2.1.2 Assign responsibilities among members. 2.1.3 Set performance expectation for team members. 2.1.4 Supervise team performance. | 3 hours |
| 3. Develop and practice negotiation skills | 3.1 Developing and practicing negotiation skills | 3.1.1 Plan negotiations 3.1.2 Participate in negotiations | 4 hours |
| 4. Solve workplace problem related to work activity | 4.1 Identifying/ determining fundamental cause of problem | 4.1.1 Explain the analytical techniques. 4.1.2 Identify the problem. 4.1.3 Determine the possible cause/s of the problem. | 4 hours |
| 5. Solve mathematical concept and techniques | 5.1 Solving mathematical concept and techniques | 5.1.1 Identify mathematical tools and techniques to solve problems. 5.1.2 Apply mathematical procedure/ solution. 5.1.3 Analyze results. | 3 hours |
| 6. Use relevant technologies | 6.1 Use relevant technologies | 6.1.1 Study/ select appropriate technology 6.1.2 Apply relevant technology. 6.1.3 Maintain/ enhance relevant technology | 3 hours |

# COMMON COMPETENCIES

(56 hours)

| UNIT OF COMPETENCY | MODULE TITLE | LEARNING OUTCOMES | NOMINAL DURATION |
| --- | --- | --- | --- |
| Apply safety practices | 1.1 Applying safety practices | 1.1.1 Identify hazardous area 1.1.2 Use personal protective clothing and devices 1.1.3 Perform safe handling of tools, equipment and materials 1.1.4 Perform first aid 1.1.5 Use Fire extinguisher | 8 hours |
| 2. Interpret drawing and sketches | 2.1 Interpreting drawing and sketches | 2.1.1 Identify standard alphabet of lines 2.1.2 Identify orthographic/ isometric views 2.1.3 Interpret standard drawing symbols, dimensional tolerances and notations | 8 hours |
| 3. Perform industry calculation | 3.1 Performing industry calculation | 3.1.1 Perform four fundamental operations. 3.1.2 Perform conversion of units 3.1.3 Perform calculations on algebraic expressions 3.1.4 Compute percentage and ratio | 8 hours |
| 4. Contribute to quality system | 4.1 Contributing to quality system | 4.1.1 Inspect work done. 4.1.2 Apply quality standards to work 4.1.3 Protect company property and customer interests | 4 hours |
| 5. Use handtools | 5.1 Using handtools | 5.1.1 Select hand tools 5.1.2 Use hand tools 5.1.3 Maintain hand tools | 4 hours |
| 6. Prepare weld materials | 6.1 Preparing weld materials | 6.1.1 Set up cutting equipment 6.1.2 Cut and prepare edge of materials 6.1.3 Clean surfaces and edges 6.1.4 Prepare welding consumables 6.1.5 Prepare welding safety and protective equipment | 8 hours |
| 7. Set-up welding equipment | 7.1 Setting-up welding equipment | 7.1.1 Set up welding machine 7.1.2 Set up welding accessories 7.1.3 Set up welding positioners, jigs and fixtures | 4 hours |
| 8. Fit-up materials | 8.1 Fitting up materials | 8.1.1 Perform tack welding 8.1.2 Check gap and alignment | 4 hours |
| 9. Repair weld | 9.1 Repairing weld | 9.1.1 Mark/locate weld defects 9.1.2 Prepare tools and equipment 9.1.3 Remove defects 9.1.4 Perform re-welding | 8 hours |

# CORE COMPETENCIES

(72 hours)

| UNIT OF COMPETENCY | MODULE TITLE | LEARNING OUTCOMES | NOMINAL DURATION |
| --- | --- | --- | --- |
| 1. Weld alloy steel plate using GMAW | 1.1 Performing fillet welding on alloy steel plate | Weld alloy steel plates in 1F position Weld alloy steel plates in 2F position Weld alloy steel plates in 3F position Weld alloy steel plates in 4F position | 16 hours |
|  | 1.2 Performing groove welding on alloy steel plate | 1.2.1 Weld alloy steel plates in flat position (IG) 1.2.2 Weld alloy steel plates in horizontal position (2G) Weld alloy steel plates in vertical position (3G) | 16 hours |
| 2. Weld alloy steel pipe using GMAW | 2.1 Performing groove welding on alloy steel pipe | 2.1.1 Weld alloy steel pipes in 2G position 2.1.2 Weld alloy steel pipes in 5G position 2.1.3 Weld alloy steel pipes in 6G position | 40 hours |

# ASSESSMENT METHODS:

- Written examination

- Demonstration of practical skills

- Direct observation

- Interview

COURSE DELIVERY:

- Modular

- Demonstration

- Lecture

- Discussion

- Dual training

RESOURCES:

| Equipment GMAW welding machine complete with accessories Welding booth Welding table or jig Stabilizing oven Tools /accessories/supplies Set of box wrench Welding mask Chipping hammer Steel brush Dark glass Clear glass Weld gauge Penlight Dye penetrant (DPT) kit Cutting / grinding disk alloy steel plates / pipes Portable oven Portable grinder Shielding gases MIG wire | Training materials Reference books Manuals Catalogs Brochures Modules/LEs CDs/Video tapes Arc welding manuals Welding standards Welding procedures specifications (WPS) Personal protective equipment safety shoes safety goggles apron gloves leggings |
| --- | --- |

# TRAINER’S QUALIFICATIONS:

- Must be a holder of Welding (GMAW) NC III.

- Must have undergone training on Training Methodology II (TM II).

- Must be computer literate.

- Must be physically and mentally fit.

- *Must have at least 2 years job/ industry experience.

- Must be a civil service eligible or appropriate professional license issued by the Professional Regulatory Commission (for government position).

* Optional: only when required by hiring institution

AS PER TESDA RESOLUTION NO. 2004-03

MODULES OF INSTRUCTION

BASIC COMPETENCIES

GAS METAL ARC WELDING (GMAW) NC III

UNIT OF COMPETENCY	:	LEAD WORKPLACE COMMUNICATION

MODULE TITLE	:	LEADING WORKPLACE COMMUNICATION

MODULE DESCRIPTOR	: 	This module covers the knowledge, skills and attitudes required to prepare different reports required in the workplace.

SUGGESTED DURATION	:	3 hours

SUMMARY OF LEARNING OUTCOMES:

Upon completion of this module the students/trainees will be able to:

LO1.	Communicate information about workplace processes.

LO2.	Lead workplace discussions.

LO3.	Identify and communicate issues arising in the workplace.

LO1.	COMMUNICATE INFORMATION ABOUT WORKPLACE PROCESSES

# ASSESSMENT CRITERIA:

- Appropriate communication method is selected.

- Multiple operations involving several topic areas are communicated.

- Questions are used to gain extra information.

- Correct sources of information are identified.

- Information is selected and sequenced correctly when required.

- Verbal and written reporting are maintained in both familiar and unfamiliar situations.

CONTENTS:

- Method of communication

- Communication skills

- Communication tools

- Questioning techniques

CONDITIONS:

The students/trainees must be provided with the following:

- Simulated workplace environment

- Communication tools

- Variety of information’s

METHODOLOGIES:

- Discussion

- Role play

- Brainstorming

ASSESSMENT METHOD:

- Direct observation

- Interview

LO2.	LEAD WORKPLACE DISCUSSIONS

# ASSESSMENT CRITERIA:

- Responses to workplace issues are sought.

- Response to workplace issues are provided when sought.

- Constructive contributions are made to workplace discussion on such issues as production, quality and safety.

- Goals and aims of actions under taken in the workplace are communicated.

CONTENTS:

- Method/techniques  of discussion

- How to lead discussion

- How to solicit response

CONDITIONS:

The students/trainees must be provided with the following:

- Simulated workplace environment

- Communication tools

- Variety of information’s

METHODOLOGIES:

- Discussion

- Role play

- Brainstorming

ASSESSMENT METHOD:

- Direct observation

- Interview

LO3.	IDENTIFY AND COMMUNICATE ISSUES ARISING IN THE WORKPLACE

# ASSESSMENT CRITERIA:

- Issues and problems are identified as they arise.

- Information regarding problems and issues are organized coherently to ensure clear and effective communication.

- Dialog is initiated with appropriate personnel.

- Communication problems and issues are addressed as they arise.

CONTENTS:

- Identify problems and issues

- Organizing information on  problem and issues

- Relating problems and issues

- Communication barriers affecting workplace discussions.

CONDITIONS:

The students/trainees must be provided with the following:

- Simulated workplace environment

- Communication tools

- Variety of information’s

METHODOLOGIES:

- Discussion

- Role play

- Brainstorming

ASSESSMENT METHOD:

- Direct observation

- Interview

UNIT OF COMPETENCY	:	LEAD SMALL TEAM

MODULE TITLE	:	LEADING SMALL TEAM

MODULE DESCRIPTOR	: 	This module covers the knowledge, skills and attitudes   required to lead small team including setting and maintaining team and individual performance standard.

SUGGESTED DURATION	:	3 hours

SUMMARY OF LEARNING OUTCOMES:

Upon completion of this module the students/trainees will be able to:

LO1.	Provide team leadership.

LO2.	Assign responsibilities among members.

LO3.	Set performance expectation for team members.

LO4.	Supervise team performance.

LO1.	PROVIDE TEAM LEADERSHIP

# ASSESSMENT CRITERIA:

- Work requirements are identified and prescribed to members.

- Reasons for instructions and requirements are properly disseminated to team members.

- Team members questions, problems, concerns are recognized, discussed and dealt accordingly.

CONTENTS:

- Communication skills required for leading small team

- Skills and techniques in promoting  team building

- Negotiating skills

- Up to date dissemination of instruction and requirements to members.

- Art of listening and treating individual team members concern

CONDITIONS:

The students/trainees must be provided with the following:

- Learning materials

- Team building manual

- Catalogs

- Brochures

- Simulated team

METHODOLOGIES:

- Traditional/ lecture

- Demonstration

- Case studies

LO2.	ASSIGN RESPONSIBILITIES AMONG MEMBERS

ASSESSMENT CRITERIA:

- Duties and responsibilities are allocated in respect to the skills, knowledge and attitudes of every team member.

- Duties are allocated having regard to individual preference, domestic and personal considerations.

- Duties and responsibilities of each member are properly identified and defined.

CONTENTS:

- Duties and responsibilities of each team member

- Skills in identifying individual skills ,knowledge  and attitude as basis for allocating responsibilities

- Knowledge in identifying each team member duties and responsibilities

CONDITIONS:

The students/trainees must be provided with the following:

- Learning materials

- Relevant legal requirements

- Manuals

METHODOLOGIES:

- Traditional/ lecture

- Demonstration

LO3.	SET PERFORMANCE EXPECTATION FOR TEAM MEMBERS

# ASSESSMENT CRITERIA:

- Performance expectations are established based on client needs and according to assigned requirements.

- Performance expectations are based on individual team member’s duties and responsibilities.

- Performance expectations are discussed and disseminated to individual team member.

CONTENTS:

- Knowledge and skills in setting individual performance target/expectation

- Team members duties  and responsibilities

- Employee policies and procedures

- Defining performance expectations criteria

CONDITIONS:

The students/trainees must be provided with the following:

- Performance expectation worksheet

- Relevant legal requirements

METHODOLOGIES:

- Traditional/ lecture

- Demonstration

- Case studies

LO4.	SUPERVISE TEAM PERFORMANCE

# ASSESSMENT CRITERIA:

- Monitor team member’s performance in respect to the defined performance criteria.

- Provide team members with feedback, positive support and advice on strategies to overcome any difficulties.

- Inform team members of any changes in the priority allocated to assignment or task.

- Provide communication follow-up on all issues affecting the team.

CONTENTS:

- Knowledge and skills in monitoring team member performance

- Monitoring team operation to ensure client needs  and satisfaction

- Methods of monitoring performance

- Informal/formal counseling skills

CONDITIONS:

The students/trainees must be provided with the following:

- Performance expectation worksheet

- Relevant legal requirements

METHODOLOGIES:

- Traditional/ lecture

- Demonstration

- Modular

ASSESSMENT METHOD:

- Written examination

- Direct observation

UNIT OF COMPETENCY	:	DEVELOP AND PRACTICE MEGOTIATION SKILLS

MODULE TITLE	:	Developing and Practicing Negotiation Skills

MODULE DESCRIPTOR	: 	This module covers the skills, knowledge and attitudes required to collect information in order to plan and participate in the negotiation.

NOMINAL DURATION	:    3 hours

SUMMARY OF LEARNING OUTCOMES:

Upon completion of this module the students/ trainees will be able to:

# LO1.	Plan negotiations

LO2.	Participate in negotiations

# LO1.	Plan Negotiations

ASSESSMENT CRITERIA:

- Information in preparation  for negotiation is identified and included in the plan

- Information on creating non verbal environments for positive negotiations  is identified and included in the plan

- Information on different questioning techniques is identified and included in the plan

CONTENTS:

- Background information on other parties to the negotiation

- Observing differences between content and process

- Identifying bargaining information

- Applying strategies to manage process

- Applying steps in negotiating process

- Strategies to manage conflict

- Steps in negotiating process

CONDITIONS:

The students/ trainees must be provided with the following:

- Pertinent documents

- Simulated workplace

- Paper and pencil

- Calculator

- Hands out

METHODOLOGIES:

- Lecturette

- Role playing

- Practical exercises

# LO2.	Participate in Negotiations

ASSESSMENT CRITERIA:

- Criteria for successful outcome are agreed upon by all parties

- Desired outcome of all parties are considered

- Appropriate language is used throughout the negotiation

- The issues and processes are documented and agreed upon by all parties

- Possible solutions are discussed and their viability assessed

- Areas for agreement are confirmed and recorded

- Follow-up action is agreed upon by all parties

CONTENTS:

- Decision making and conflict resolution strategies procedures

- Problem solving strategies on how to deal with unexpected questions and attitudes during negotiation

- Background information on other parties to the negotiation

- Observing differences between content and process

CONDITIONS:

The students/ trainees must be provided with the following:

- Pertinent documents

- Simulated workplace

- Paper and pencil

- Calculator

- Hands out

METHODOLOGIES:

- Lecturette

- Role playing

- Practical exercises

ASSESSMENT METHODS:

- Written test/ questioning

- Demonstration

UNIT OF COMPETENCY	:	SOLVE WORKPLACE PROBLEM RELATED TO WORK ACTIVITIES

MODULE TITLE	:	IDENTIFYING/ DETERMINING FUNDAMENTAL CAUSE OF PROBLEM

MODULE DESCRIPTOR	: 	This module expresses the competency required to apply problem solving techniques to identify/determine fundamental cause problem.

SUGGESTED DURATION	:	4 hours

SUMMARY OF LEARNING OUTCOMES:

Upon completion of this module the students/trainees will be able to:

LO1.	Explain the analytical techniques.

LO2.	Identify the problem.

LO3.	Determine the possible cause /s of the problem.

LO1.	EXPLAIN THE ANALYTICAL TECHNIQUES

# ASSESSMENT CRITERIA:

- Importance and application of analytical techniques are explained.

- Analytical techniques such as brainstorming, cause and effects diagrams, PARETO analysis, SWOT analysis, GANT chart, PERT CPM & graphs, and scatter grams are defined.

CONTENTS:

- Observation, investigation & analytical techniques

- Brainstorming

- Cause and effect diagrams

- PARETO analysis

- SWOT analysis

- GANT chart

- PERT CPM & graph

- SCATTERGRAMS

CONDITIONS:

The students/trainees must be provided with the following:

- Coursewares

- Learning materials/guides

- Computer

- OHP

METHODOLOGIES:

- Direct observation

- Simulation /role playing

- Case studies

ASSESSMENT METHOD:

- Written

- Practical/performance test

LO2.	IDENTIFY THE PROBLEM

# ASSESSMENT CRITERIA:

- Variances are identified from normal operating parameters and product quality.

- Extent, cause, and nature of the problem are defined based on observation, investigation and analytical techniques.

- Problems are clearly stated and specified.

CONTENTS:

- Normal operating parameters & product quality

- Identifying & clarifying the nature of problem

- Application of analytical techniques

CONDITIONS:

The students/trainees must be provided with the following:

- Coursewares

- Learning materials/guides

- Computer

- OHP

METHODOLOGIES:

- Direct observation

- Simulation /role playing

- Case studies

ASSESSMENT METHOD:

- Written

- Practical/performance test

LO3.	DETERMINE THE POSSIBLE CAUSE/S OF THE PROBLEM

# ASSESSMENT CRITERIA:

- Possible cause/s of problem are identified based on experience & the use of problem solving tools/analytical techniques.

- Possible cause statements are developed.

- Fundamental causes are explained.

CONTENTS:

- Non-routine process and quality problems

- Teamwork and work allocation problem

- Safety and emergency situations and incidents

CONDITIONS:

The students/trainees must be provided with the following:

- Coursewares

- Learning materials/guides

- Computer

- OHP

METHODOLOGIES:

- Direct observation

- Simulation /role playing

- Case studies

ASSESSMENT METHOD:

- Written

- Practical/performance test

UNIT OF COMPETENCY	:	USE MATHEMATICAL CONCEPTS AND TECHNIQUES

MODULE TITLE	:	USING MATHEMATICAL CONCEPTS AND TECHNIQUES

MODULE DESCRIPTOR	:	This unit covers the knowledge, skills and attitudes required in the application of mathematical concepts and techniques.

NOMINAL DURATION	:	4 hours

SUMMARY OF LEARNING OUTCOMES:

Upon completion of the module, the learner/students must be able to:

LO1.	Identify mathematical tools and techniques to solve problems.

LO2.	Apply mathematical procedure/solution.

LO3. 	Analyze results.

LO1.	Identify mathematical tools and techniques to solve problems

# ASSESSMENT CRITERIA:

- Problem areas based on given condition are identified.

- Mathematical techniques based on the given problem are selected.

# CONTENTS:

- Four fundamental operations

- Steps in solving a problem

- Standard formulas

- Conversion

- Measurement

# CONDITION:

# The students/learners must be provided with the following:

- Manuals

- Hand-outs

- Problem set

- Conversion table

- Table of formulas

- Measuring tools

# METHODOLOGIES:

- Lecturette

- Self-pace

- Group discussion

# ASSESSMENT METHODS:

- Written

- Demonstration

LO2.	Apply mathematical procedure/solution

# ASSESSMENT CRITERIA:

- Mathematical techniques based on the problem identified are applied.

- Mathematical computations are performed to the level of accuracy required for the problem.

- Results of mathematical computation based on job requirements is determined and verified.

# CONTENTS:

- Problem-based questions

- Estimation

- Use of mathematical tools and standard formulas

- Mathematical techniques

# CONDITION:

# The students/learners must be provided with the following:

- Manuals

- Hand-outs

- Calculator

- Measuring tools/devices

- Case problems

# METHODOLOGIES:

- Lecturette

- Self-pace

- Group discussion

- Practical Work Approach

# ASSESSMENT METHODS:

- Written

- Oral Interview

LO3.	ANALYZE RESULTS

# ASSESSMENT CRITERIA:

  - Results of application based on expected and required specifications and outcome is reviewed.

  - Appropriate action in case of error is applied.

# CONTENTS:

- Four fundamental operations

- Steps in solving a problem

- Standard formulas

- Conversion

- Measurement

# CONDITION:

# The students/learners must be provided with the following:

- Manuals

- Hand-outs

- Problem set

- Conversion table

- Table of formulas

- Measuring tools

# METHODOLOGIES:

- Lecturette

- Self-pace

- Group discussion

- Research study

# ASSESSMENT METHODS:

- Written

- Oral

##### UNIT OF COMPETENCY	:	USE RELEVANT TECHNOLOGIES

##### MODULE TITLE                 :	USING RELEVANT TECHNOLOGIES

MODULE DESCRIPTOR	:	This unit covers the knowledge, skills and attitudes required in selecting, sourcing and applying appropriate and affordable technologies in the workplace.

NOMINAL DURATION	:	3 hours

SUMMARY OF LEARNING OUTCOMES:

Upon completion of the module, the learner/students must be able to:

LO1.	Study/ select appropriate technology

LO2.	Apply relevant technology.

LO3.	Maintain/ enhance relevant technology

LO1.	Study/ select appropriate technology

ASSESSMENT CRITERIA:

- Appropriate technology are studied based on work requirements.

- Appropriate technology are identified and selected based on work requirements.

CONTENTS:

- Machineries/ equipment and their application

- Software/ programs

CONDITION:

The students/learners must be provided with the following:

- Manuals

- Hand-outs

- Multimedia

- Video tape

- Brochures

- CD’s

- Internet access

- Computer

METHODOLOGIES:

- Lecturette

- Self-pace

- Group discussion

- Film showing

ASSESSMENT METHODS:

- Written

- Interview

LO2.	Apply relevant technology

# ASSESSMENT CRITERIA:

1.	Relevant technology is used in carrying out function based on work requirements.

2.	Applicable software and hardware is used as per job requirement.

3. 	Management concept are observed as per established industry practices.

CONTENTS:

- Office technology

- Industrial technology

- System technology

- Information technology

- Training technology

- Different software/ hardware

- 5S (proper house keeping)

CONDITION:

The students/learners must be provided with the following:

- Manuals

- Hand-outs

- Multimedia

- Video tape

- Brochures

- CD’s

- Internet access

- Computer

METHODOLOGIES:

- Lecturette

- Self-pace

- Group discussion

- Film showing

ASSESSMENT METHODS:

- Written

- Interview

LO3.	MAINTAIN/ ENHANCE RELEVANT TECHNOLOGY

# ASSESSMENT CRITERIA:

- Maintenance of technology is applied in accordance with the industry standard operating procedure, manufacturer’s operating guidelines and occupational health and safety procedure

- Updating of technology is maintained through continuing education or training in accordance with job requirement.

- Appropriate action for technology failure/ defect is immediately reported to the concerned/ responsible person or section.

# CONTENTS:

- Corrective and preventive maintenance

- Upgrading of technology

- Communication Skills

- Organizational set-up/ work flow

# CONDITION:

# The students/learners must be provided with the following:

- Manuals

- Hand-outs

- Multimedia

- Video tape

- Brochures

- CD’s

- Internet access

- Computer

# METHODOLOGIES:

- Lecturette

- Self-pace

- Group discussion

- Film showing

# ASSESSMENT METHODS:

- Written

- Interview

MODULES OF INSTRUCTION

COMMON COMPETENCIES

GAS METAL ARC WELDING (GMAW) NC III

UNIT OF COMPETENCY	: 	APPLY SAFETY PRACTICES

# MODULE TITLE	:	Applying safety practices

MODULE DESCRIPTION	: 	This module covers safety practices applied in the workplace.

SUGGESTED DURATION	:	4 hours

SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

### LO1.	Identify hazardous area

### LO2.   Use personal protective clothing and devices

### LO3.	Perform safe handling of tools, equipment and materials

### LO4.	Perform first aid

### LO5.	Use Fire extinguisher

### LO1.	IDENTIFY HAZARDOUS AREA

### ASSESSMENT CRITERIA:

- Hazards are identified correctly in accordance with OHS procedures.

- Safety signs and symbols are identified and adhered to in accordance with workplace safety procedure.

### CONTENTS:

  - Hazard to be avoided in welding

  - Welding safety signs and symbols

  - Occupational safety standards and enterprise safety policies.

### CONDITION:

The students/ trainee should be provided with:

  - Safety sign and symbols

  - Instructional materials

-	Reference book

-	Learning modules/manuals

-	Safety standards manual

-	Enterprise safety policies/guidelines

### METHODOLOGIES:

  - Lecture/demonstrations

  - Self pace learning

  - Group discussion

### ASSESSMENT METHODS:

  - Written/oral

  - Direct observation

  - Interview

### LO2.	USE PERSONAL PROTECTIVE CLOTHING AND DEVICES

### ASSESSMENT CRITERIA:

- Personal protective clothing/equipment (PPE) identified as per job requirements

- Proper wearing of PPE are properly observed in accordance with workplace safety policies.

- PPE conformed with the approved occupational safety standards.

### CONTENTS:

- Personal protective equipment (PPE) for different welding operations

- Proper uses of different types of personal protective equipment (PPE)

- Occupational safety standards and enterprise safety policies.

### CONDITION:

### The students/ trainee should be provided with:

- Personal protective equipment (PPE)

-	Hard hat

-	Safety shoes

-	Gloves

-	Goggles

-	Welder apron

- Instructional materials for:

-	Reference book

-	Learning modules/manuals

-	Safety standards

-	Enterprise safety policies/guidelines

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

### LO3.	PERFORM SAFE HANDLING OF TOOLS, EQUIPMENT AND MATERIALS

### ASSESSMENT CRITERIA:

- Pre-use checking and inspection of tools and equipment are conducted in accordance with industry/ company policies.

- Safe handling of tools, equipment and materials are properly observed in accordance with OHS requirements and industry/ company policies.

- Safety label and tag of tools and equipment are strictly followed in accordance with industry/ company policies.

### CONTENTS:

- Pre-use inspection and checking procedure

- Safe handling of tools, equipment and materials

- Equipment and power tools orientation and familiarization

- Workplace Occupational Health and Safety procedures

### CONDITION:

### The students/ trainee should be provided with:

- Equipment/accessories

-	Hard hat

- 	Safety shoes

- 	Gloves

- 	Goggles

- 	Welder apron

- Instructional materials:

-	Reference book

-	Learning modules/manuals

-	Safety standards

-	Enterprise safety policies/guidelines

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

### LO4.	PERFORM FIRST AID

### ASSESSMENT CRITERIA:

- First aid treatment of injuries are carried out according to recommended procedures

- Emergency hotline and proper authority are accessed and contacted in accordance with workplace procedure.

### CONTENTS:

- Different types of injuries

- First aid treatment procedure

- Emergency hotline number and offices

- Proper handling of injured individual

### CONDITION:

### The students/ trainee should be provided with:

- Equipment

-	First aid kit (different types)

-	Oxygen

-	Stretcher

-	Medicine

- Learning materials

-	Video tape, CD’s, transparencies

- Directory hotline number and offices

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO5.	USE FIRE EXTINGUISHER

### ASSESSMENT CRITERIA:

- Fire fighting equipment identified according to types/source of fires.

- Use of fire fighting equipment demonstrated in accordance with manufacturer’s instructions.

- Used fire fighting equipment and accessories are recorded/reported for replacement/refill in accordance with enterprise approved safety regulations.

### CONTENTS:

- Types of fire fighting equipment

- Types of fire extinguishers

- Fire hoses

- Fire hydrants

- Sources/causes of fires

- Proper use of fire fighting equipment

### CONDITION:

### The students/ trainee should be provided with:

- Equipment

-	Fire extinguishers (different types)

-	Fire hydrants

-	Video players/monitors

- Learning materials

-	Types of fires/sources

-	Types of fire fighting equipment and its operations

-	Manuals on fire protection regulations

-	Video tape, CD’s, transparencies

-	Report cards/checklist

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

UNIT OF COMPETENCY	: 	INTERPRET DRAWINGS AND SKETCHES

# MODULE TITLE	:  	Interpreting drawing and sketches

MODULE DESCRIPTION	:	This module covers knowledge, skills and attitudes required to interpret drawing and sketches in accordance with work plan specifications.

### SUGGESTED DURATION	:	8 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Identify standard alphabet of lines

LO2.	Identify orthographic/ isometric views

LO3.   Interpret standard drawing symbols, dimensional tolerances and notations

LO1.	IDENTIFY STANDARD ALPHABET OF LINES

### ASSESSMENT CRITERIA:

- Alphabet of lines identified according to ISO.

2.	Alphabet of lines are clearly explained according to their use.

### CONTENTS:

- Alphabet of lines and applications

- Drawing specifications

- Dimensions

- Scaling

### CONDITION:

### The students/ trainee should be provided with:

- Equipment/accessories

-	OHP/transparencies

-	Computer

-	Video/multi-media materials

- Training materials

-	Reference book,

-	Learning modules

-	Blueprint (sample)

-	Writing instrument

-	Drawing instrument

### METHODOLOGIES:

- Lecture/demonstrations

- Self-paced instruction

- Presentation

### ASSESSMENT METHODS:

- Written

- Direct observation

- Interview/oral

### LO2.	IDENTIFY ORTHOGRAPHIC/ ISOMETRIC VIEWS

### ASSESSMENT CRITERIA:

- Orthographic and isometric views are clearly explained

- Orthographic and isometric drawing are identified based on plan

### CONTENTS:

- Types of welding joints and symbols

- Welding positions, codes and plan specifications

- Contour symbols

- Drawing technique

- Perspective

  - Exploded view

  - Hidden view technique

- Projections

  - First angle projections

  - Third angle projections

### CONDITION:

The students/ trainee should be provided with:

- Equipment/accessories

-	OHP/transparencies

-	Computer

-	Video/multi-media materials

- Training materials

-	Reference book,

-	Learning modules

-	Blueprint (sample)

-	Writing instrument

-	Drawing instrument

### METHODOLOGIES:

- Lecture/demonstrations

- Self-paced instruction

- Presentation

### ASSESSMENT METHODS:

- Written

- Direct observation

- Interview/oral

### LO3.	INTERPRET STANDARD DRAWING SYMBOLS, DIMENSIONAL TOLERANCES

### AND NOTATIONS

### ASSESSMENT CRITERIA:

- Drawing symbols are interpreted according to drawing standards

- Dimensional tolerances, notations are interpreted according to specifications

### CONTENTS:

- Types of welding joints and symbols

- Welding positions, codes and plan specifications

- Contour symbols

- Welding process (abbreviation)

### CONDITION:

### The students/ trainee should be provided with:

- Equipment/accessories

-	OHP/transparencies

-	Computer

-	Video/multi-media materials

- Training materials

-	Reference book,

-	Learning modules

-	Blueprint (sample)

-	Writing instrument

-	Drawing instrument

### METHODOLOGIES:

- Lecture/demonstrations

- Self-paced instruction

- Presentation

### ASSESSMENT METHODS:

- Written

- Direct observation

- Interview/oral

UNIT OF COMPETENCY	:  	PERFORM INDUSTRY CALCULATION

# MODULE TITLE	: 	Performing Industry Calculation

MODULE DESCRIPTION	: 	This module covers knowledge, skill and attitude required to compute/calculate quantity /size/cost of materials/parts, and convert systems of measurements using formulas and other methods.  This also includes measuring instruments and its applications.

SUGGESTED DURATION	:	8 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Perform four fundamental operations.

LO2.	Perform conversion of units

LO3.	Perform calculations on algebraic expressions

LO4.	Compute percentage and ratio

### LO1.	PERFORM FOUR FUNDAMENTAL OPERATION

### ASSESSMENT CRITERION:

### Simple calculations involving whole numbers, mixed numbers, fraction and decimal are performed using four fundamental operations

### CONTENTS:

- Mathematical operations

- subtraction

- addition

- multiplication

- division

- Industrial mathematics

- Computation formulas finding areas of:

- plane

- circles

- triangles

- other geometrical figures

### CONDITION:

### The students/ trainee should be provided with:

- Equipment/ accessories

-	Calculators

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO2.	PERFORM CONVERSION UNIT

### ASSESSMENT CRITERIA:

1.	Units are converted to the required figure using the given formulae

#### 2.	English measurements are converted to metric measurements according to procedure.

### CONTENTS:

- Units

-	Fractions

-	Mixed numbers

-	Decimal

- Conversion of English to metric (vise versa)

### CONDITION:

### The students/ trainee should be provided with:

- Equipment/ accessories

-	Calculators

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO3.	PERFORM CALCULATIONS ON ALGEBRAIC EXPRESSIONS

### ASSESSMENT CRITERIA:

      - Simple calculations are performed on algebraic expressions using the four fundamental operations

      - Simple transposition of formulae are carried out to isolate the variable required, involving the four fundamental operations.

      - Appropriate formula applied and results obtained in accordance with job specifications.

### CONTENTS:

- English and metric system of measurements

- Four fundamental operations

- Method of transposing formulae

- Equation formulation

### CONDITION:

### The students/ trainee should be provided with:

- Equipment/ accessories

-	Calculators

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO4.	COMPUTE PERCENTAGE AND RATIO

### ASSESSMENT CRITERIA:

1.	Percentages are computed using appropriate formula.

2.	Ratio and proportion are computed using appropriate formula.

### CONTENTS:

- Ratio and proportion

- Calculation

- Percentage and ratio

### CONDITION:

### The students/ trainee should be provided with:

- Equipment /accessories

-	Calculators

- Supplies/materials

-	Pencil/paper

-	Reference books

-	Learning materials/module

-	OHP/transparencies

-	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

UNIT OF COMPETENCY	:  	CONTRIBUTE TO QUALITY SYSTEM

# MODULE TITLE	: 	Contributing to quality system

MODULE DESCRIPTION	: 	This modules covers knowledge, skill and attitude required to inspect work against specification and standards and apply quality standards to work.

SUGGESTED DURATION	:	4 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Inspect work done.

LO2.	Apply quality standards to work

LO3.	Protect company property and customer interests

### LO1.	INSPECT WORK DONE

### ASSESSMENT CRITERIA:

        - Appropriate inspections are conducted to ensure company quality systems and procedures are maintained/ followed.

2.	Job specifications/work order and quality standards are identified.

3.	Faults/defects are identified and rectified according to company procedures.

### CONTENTS:

- Quality system and procedures

-	Work instructions

-	Safe work procedures

-	Product specifications

-	Equipment maintenance schedules

-	Technical procedures adopted or specifically prepared standards

-	Company/industry rules

- Faults and defects

- Communication/feedback methods-written and verbal

### CONDITION:

### The students/ trainee should be provided with:

- Inspection record manual

- Job specification

- Workplace/company procedure manual

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO2.	APPLY QUALITY STANDARDS TO WORK

### ASSESSMENT CRITERIA:

- Inspections are conducted throughout the manufacturing processes to ensure quality standards are maintained.

- Appropriate quality standards are applied throughout the production/fabrication process.

- All activities are coordinated throughout the workplace to ensure efficient quality work outcomes.

### Records of work quality are maintained according to the company requirements

### CONTENTS:

- Quality standard/ISO

- Work inspection techniques/procedures

- Record maintenance

- Communication process

### CONDITION:

### The students/ trainee should be provided with:

- Inspection record manual

- Quality standard

- Job specification

- Workplace/company procedure manual

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO3.	PROTECT COMPANY PROPERTY AND CUSTOMER INTERESTS

### ASSESSMENT CRITERIA:

  - Possible damage to company property is avoided by adherence to company quality procedures.

  - Quality of work is reviewed to ensure customer requirements and company standards are met.

### CONTENTS:

- Company systems, processes and work quality requirements

- Quality assurance principles

- Safety precautionary measures

- Handling materials, tools and equipment

### CONDITION:

The students/ trainee should be provided with:

- Inspection record manual

- Quality standard

- Job specification

- Workplace/company procedure manual

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

UNIT OF COMPETENCY	:	USE HAND TOOLS

# MODULE TITLE                 :	Using hand tools

MODULE DESCRIPTION	:	This modules covers knowledge skills and attitude required to use hand tools

SUGGESTED DURATION	:	4 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Select hand tools

LO2.	Use hand tools

LO3.	Maintain hand tools

### LO1.	SELECT HAND TOOLS

### ASSESSMENT CRITERIA:

- Hand tools selected are appropriate to the requirements of the task.

### Unsafe or defective tools are identified and marked for repair according to procedure

### CONTENTS:

- Types and uses of hand tools

- Hand tool defects

### CONDITION:

### The students/ trainee should be provided with:

- Hand tools

  - Hacksaws

  - Hammers (ball peen, chipping)

  - Punches

  - Screwdrivers

  - Wrenches

  - Scrapers

  - Chisels

  - Gouges

  - Files

  - Clamps

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO2.	USE HAND TOOLS

### ASSESSMENT CRITERIA:

    - Hand tools are used to produce the desired outcomes to job specifications.

### Task performed in accordance with company or industry safety procedure

### CONTENTS:

- Types and uses of hand tools

- Tasks:

- Adjusting

- Dismantling

- Assembling

- Finishing of item or components

### CONDITION:

### The students/ trainee should be provided with:

- Hand tools

  - Hacksaws

  - Hammers (ball peen, chipping)

  - Punches

  - Screwdrivers

  - Wrenches

  - Scrapers

  - Chisels

  - Gouges

  - Files

  - Clamps

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO3.	MAINTAIN HAND TOOLS

### ASSESSMENT CRITERIA:

  - Routine maintenance of hand tools is undertaken according to standard operating procedures, principles and techniques.

  - Hand tools are stored in designated location in accordance with manufacturer’s instruction/standard operating procedure.

### CONTENTS:

- Routine maintenance

  - Lubricating

  - Tightening

  - Simple tool repair

  - Hand sharpening

  - Cleaning

- Proper storage of hand tools

### CONDITION:

### The students/ trainee should be provided with:

- Hand tools

  - Hacksaws

  - Hammers (ball peen, chipping)

  - Punches

  - Screwdrivers

  - Wrenches

  - Scrapers

  - Chisels

  - Gouges

  - Files

  - Clamps

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Demonstration

UNIT OF COMPETENCY	:	PREPARE WELD MATERIALS

# MODULE TITLE                 :	Preparing weld materials

MODULE DESCRIPTION	: 	This modules covers knowledge, skills and attitude required in preparing weld materials.

SUGGESTED DURATION	:	8 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Set up cutting equipment

LO2.	Cut and prepare edge of materials

LO3.	Clean surfaces and edges

LO4.	Prepare welding consumables

LO5.	Prepare welding safety and protective equipment

### LO1.	SET UP CUTTING EQUIPMENT

### ASSESSMENT CRITERIA:

- Cutting equipment should be operational and should conform to acceptable OH&S standards

- Cutting equipment fittings, connection and power source are checked in accordance with workplace procedure

### CONTENTS:

- Parts and function of cutting equipment

- Procedures in setting–up of cutting equipment

- Procedure in checking cutting equipment functionality.

### CONDITION:

### The students/ trainee should be provided with:

- Hand tools

- Cutting equipment and accessories

- Gases (oxygen, acetylene, LPG)

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO2.	CUT AND PREPARE EDGE OF MATERIALS

### ASSESSMENT CRITERIA:

- Materials are cut to specified dimension/specifications.

- Task are performed in accordance with company/industry requirement and safety procedure

### CONTENTS:

- Cutting operation procedure

- Cutting material with different process

-	Oxy-acetylene gas cutting equipment (manual and automatic)

-	Plasma cutting equipment

-	Shearing machine

-	Disc cutter

-	Cutting electrode

CONDITION:

The students/ trainee should be provided with:

- Hand tools

- Cutting equipment and accessories

- Gases (oxygen, acetylene, LPG)

- Air compressor

- Shearing machine

- Disc cutter

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Demonstration

### LO3.	PREPARE WELDING CONSUMABLES

ASSESSMENT CRITERIA:

  - Consumables, materials, specified and quantity determined in accordance with job requirements.

  - Correct materials selected in accordance with job requirements.

CONTENTS:

- Consumable materials specifications

- Equipment and tools for preparing plates and pipes edges

- Safe working practices in preparing consumables

CONDITION:

The students/ trainee should be provided with:

- Hand tools

- Cutting equipment and accessories

- Gases (oxygen, acetylene, LPG)

- Air compressor

- Shearing machine

- Disc cutter

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Demonstration

### LO4.	CLEAN SURFACES AND EDGES

ASSESSMENT CRITERIA:

  - Surfaces are cleaned to required specifications.

  - Task performed in accordance with company or industry requirements and safety procedure

CONTENTS:

- Procedures and techniques of preparing plates and pipe edges for welding

- Equipment and tools for preparing plates and pipes edges

- Safe working practices

CONDITION:

The students/ trainee should be provided with:

- Hand tools

- Cutting equipment and accessories

  - Mild steel

  - Carbon steel

  - Alloy steel

  - Cutting gases

  - Gouging electrodes

  - Grinding/cutting discs

  - Run on/run off, backing plates/ring

- Shearing machine

- Disc cutter

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Demonstration

### LO5.	PREPARE WELDING SAFETY AND PROTECTIVE EQUIPMENT

ASSESSMENT CRITERIA:

  - PPE should conform to acceptable OH&S requirement and standards.

  - Welding safety and protective equipment are checked in accordance with safety procedure

CONTENTS:

- Procedures and techniques in checking protective equipment

- Safe working practices and handling of protective equipment

CONDITION:

The students/ trainee should be provided with:

- Personal protective equipment

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Demonstration

# UNIT OF COMPETENCY	:	SET-UP WELDING EQUIPMENT

# MODULE TITLE                 : 	SETTING-UP WELDING EQUIPMENT

MODULE DESCRIPTION	:	This modules covers knowledge, skills and attitude required in setting up welding   equipment.

SUGGESTED DURATION	:	4 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Set up welding machine

LO2.	Set up welding accessories

LO3.	Set up welding positioners, jigs and fixtures

LO1.	SET UP WELDING MACHINE

### ASSESSMENT CRITERIA:

- Primary cable attached to welding machine primary cable terminal

- Primary cable attached to power source.

- Welding machine checked for functionality.

- Polarity switch, if any, set to DC reverse.

- Cable terminals checked for tightness.

### CONTENTS:

- Parts and function of welding machine  (SMAW)

- Procedures in setting –up of welding machines

- Procedure in checking welding machine functionality.

### CONDITION:

The students/ trainee should be provided with:

- Equipment and accessories

-	AC/DC Welding machine

-	Welding cables

- Ground clamp

-	Primary cable

- Power source  connectors and outlets

- Tools

-	Set of screw driver

-	Set of wrenches

- Supplies/materials

- 	Electrical tape

-  	Rubber tape

- Instructional  materials

-	Reference book /modules/ learning guides/ video CDs

- 	Equipment manual

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO2.	SET UP WELDING ACCESSORIES

### ASSESSMENT CRITERIA:

    - Electrode cable connected to positive of welding machine.

    - Ground cable connected to negative terminal of welding machine.

    - Ground clamp attached to workpiece/material.

    - Welding cable checked for crack, burns and cuts.

    - Primary cable attached to welding machine primary cable terminal

### CONTENTS:

- Parts and function of welding machine accessories and consumables

- Procedures in setting-up of welding accessories

- Procedure in checking welding machine functionality.

### CONDITION:

### The students/ trainee should be provided with:

- Equipment and accessories

-	AC/DC Welding machine

-	Welding cables

- Ground clamp

-	Primary cable

- Power source connectors and outlets

- Tools

-	Set of screw driver

-	Set of wrenches

- Supplies/Materials

- 	Electrical tape

-	Rubber tape

- Instructional  materials

-	Reference book /modules/ learning guides/ video CDs,

- 	Equipment manual

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO3.	SET UP WELDING POSITIONER, JIGS AND FIXTURES

### ASSESSMENT CRITERIA:

  - Braces, stiffeners, rails and other jigs are provided and in conformity with job requirements.

  - Work items/materials are protected from strong winds, drafts and rainfall

### CONTENTS:

- Types of welding positioner, jigs and fixture

- Different kind of jigs and fixture

- Uses and function of welding positioner, jigs and fixture

### CONDITION:

The students/ trainee should be provided with:

- Welding positioner

- Jigs and fixture

- Tools

- Supplies/materials

- Instructional  materials

-	Reference book /modules/ learning guides/ video CDs,

- 	Equipment manual

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

# UNIT OF COMPETENCY	:	FIT UP WELD MATERIALS

# MODULE TITLE                 : 	FITTING UP WELD MATERIALS

MODULE DESCRIPTION	:	This modules covers knowledge, skills and attitude required in fitting up weld materials.

SUGGESTED DURATION	:	4 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Perform tack welding

LO2.	Check gap and alignment

### LO1.	PERFORM TACK WELDING

### ASSESSMENT CRITERIA:

- Tack welding is performed in accordance with the welding procedure requirements

- Joints are free from rust, paints, grease and other foreign materials prior to fit up or tacking.

### CONTENTS:

- Kind of tacking

- Welding procedure standard requirement

- Codes and specification

### CONDITION:

### The students/ trainee should be provided with:

- Welding machine equipment and accessories

  - Tools

  - Supplies/materials

  - Personal protective equipment

  - Drawing plan and specification

  - Instructional  materials

-	Reference book/ modules/ learning guides/ video CDs

- 	Equipment manual

### METHODOLOGIES:

  - Lecture/demonstrations

  - Self pace learning

  - Group discussion

### ASSESSMENT METHODS:

  - Written/oral

  - Direct observation

  - Interview

  - Demonstration

### LO2.	CHECK GAP AND ALIGNMENT

### ASSESSMENT CRITERIA:

  - Root gap is prepared/checked in accordance with WPS  requirements

  - Alignment of work piece are checked in accordance with welding standard

  - Included angle are checked in accordance with WPS

### CONTENTS:

- Fit up tolerances

- Workpiece alignment procedure

- Fit up

### CONDITION:

The students/ trainee should be provided with:

- Measuring tools

- Work piece

- Personal protective equipment

- Drawing plan and specification

- Instructional  materials

-	Reference book /modules/ learning guides/ video CDs,

- 	Equipment manual

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

# UNIT OF COMPETENCY	:	REPAIR WELD

# MODULE TITLE                 : 	REPAIRING WELD

MODULE DESCRIPTION	:	This modules covers knowledge, skills and attitude required in repairing weld.

SUGGESTED DURATION	:	8 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Mark/locate weld defects

LO2.	Prepare tools and equipment

LO3.	Remove defects

LO4.	Perform re-welding

### LO1.	MARK/LOCATE WELD DEFECTS

### ASSESSMENT CRITERIA:

- Location of weld defects identified/determined in accordance with industry standard.

- Weld defects marked for repair in accordance with industry standard.

- Procedures in locating weld defects performed as per approved procedures.

### CONTENTS:

- Types of welding defects

- Procedures in locating weld defects

- Proper uses of NDT equipment or tools

### CONDITION:

The students/trainees must be provided with:

- Equipment and accessories

- Tools

-	Chipping hammer

-	Steel brush

- Supplies/materials

-	Carbon steel plates

-	Pipe; alloy pipe

- Instructional materials

-  	Reference book/ modules/ learning guides/ video CDs,

-	Welding charts

-   	Work plans

-    Drawing and specifications relevant to the task

### METHODOLOGIES:

- Lecture/ demonstrations

- Self-paced learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Return demonstration

### LO2.	PREPARE TOOLS AND EQUIPMENT

### ASSESSMENT CRITERIA:

- Tools and equipment are prepared appropriate to the job requirements

- Tools and equipment are properly checked to the job requirements

### CONTENTS:

  - Tools and equipment and their uses

  - Procedures in checking tools and equipment

### CONDITION:

The students/trainees must be provided with:

  - Equipment and accessories

  - Tools

-	Chipping hammer

-	Steel brush

-	Electric grinders

  - Supplies/Materials

- Carbon steel plates

- Cutting/ grinding disk

- Carbon steel plates

- Pipe

  - Instructional materials

-	Reference book/ modules/ learning guides/ video CDs,

-	Welding charts,

-	Work plans

-    Drawing and specifications relevant to the task

### METHODOLOGIES:

  - Lecture/ demonstrations

  - Self-paced learning

  - Group discussion

### ASSESSMENT METHODS:

  - Written/oral

  - Direct observation

  - Return demonstration

### LO3.	REMOVE DEFECTS

### ASSESSMENT CRITERIA:

- Weld defects removed/excavated in accordance with welding procedures.

- Removal of non-defective welds is minimized and cleaned.

- Visual and dye-penetrant test are performed to verify the extent of removal of defects

### CONTENTS:

- Dye penetrant testing principle and applications.

- Procedures of dye penetrant testing

- Weld defects removal and excavation

### CONDITION:

The students/trainees must be provided with:

- Tools

- Chipping hammers

- Steel brush

- Supplies/materials

- Developer

- Penetrant

- Cleaner

-	Cloth/ clean rag

- Instructional materials

-	Reference book/ modules/ learning guides/ video CDs

-   	Welding charts

-   	Work plans

-  	Drawing and specifications relevant to the task

### METHODOLOGIES:

- Lecture/ demonstrations

- Self-paced learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Return demonstration

### LO4.	PERFORM RE-WELDING

### ASSESSMENT CRITERIA:

- Re-welding performed in accordance with approved repair procedure.

- No new weld defects or damages occurred during re-welding.

- Weld visually checked after re-welding for acceptability

### CONTENTS:

- Rectifying weld defects

- Re-welding procedures

- Visual inspection of weld

### CONDITION:

The students/trainees must be provided with:

- Equipment and accessories

-	Welding machine with complete accessories

- Tools

-	Chipping hammers

-	Steel brush

-	Electric grinders

- Welding supplies/materials

-	Carbon steel plates

-	Cutting/ grinding disk

-	Welding consumables

### METHODOLOGIES:

- Lecture/ demonstrations

- Self-paced learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Return demonstration

MODULES OF INSTRUCTION

CORE COMPETENCIES

GAS METAL ARC WELDING (GMAW) NC III

UNIT OF COMPETENCY	:	Weld ALLOY Steel PLATES USING GMAW

MODULE TITLE	:	Performing Groove Welding on alloy Steel Plates

MODULE DESCRIPTOR	: 	This module covers the knowledge, skills and attitude in performing groove welding on alloy steel plates in different positions such as 1G, 2G, & 3G and 1F, 2F, 3F & 4F.

NOMINAL DURATION	:	16 hours

SUMMARY OF LEARNING OUTCOMES:

Upon completion of this module the trainee/student must be able to:

LO1.	Weld alloy steel plates in flat position (1G)

LO2.	Weld alloy steel plates in horizontal position (2G)

LO3.	Weld alloy steel plates in vertical position (3G)

LO1.	Weld Alloy Plates in Flat Position (1G)

ASSESSMENT CRITERIA:

- Root penetration not exceeding allowable tolerances specified by welding codes/ standards on

- excess penetration

- lack of fusion

- burn-through

- Weld capping/ final pass not exceeding allowable tolerances specified by welding codes/ standards on

- height of reinforcement

- underfill

- porosities

- undercut

- cracks

- cold laps

- Uniformity of bead ripples must be in accordance with welding standards

- Stringer or layered beads deposited in accordance with welding standards

- Finish weldment visually acceptable in accordance with welding standards for:

- spatters

- arc strikes

- slag

- uniformity of beads

CONTENTS:

- Essentials of welding

- International welding codes and standards

- Acceptable weld profiles

- Weld defects, causes and remedies

- Welding procedure specifications (WPS)

- Welding techniques and procedures

- Safe welding practices

CONDITIONS:

The student/trainee must be provided with the following:

1.	Equipment

- GMAW welding machine (AC/DC)

- Welding table or jig

- Portable grinder

- Welding booth

2.	Tools/ accessories

- Welding mask

- Steel brush

- Clear glass

- Chipping hammer

- Dark glass

3.	Supplies/ materials

- MIG wire

- Alloy steel plates

- Cutting grinding disk

      - Shielding gases

4.	Personal protective equipment

- Safety shoes

- Apron

- Leggings

- Safety goggles

- Gloves

5.	Training materials

- GMAW welding manuals

- Welding procedures specifications (WPS)

- Welding standards

METHODOLOGIES:

- Lecture/demonstration

- Dualized

- Self-paced learning

ASSESSMENT METHODS:

- Written/oral

- Interview

- Direct observation

LO2.	Weld alloy Steel Plates in Horizontal Position (2G)

ASSESSMENT CRITERIA:

- Root penetration not exceeding allowable tolerances specified by welding codes/ standards on

- concavity

- convexity

- undercut

- excess penetration

- lack of fusion

- burn-through

- cracks

- Weld capping/ final pass not exceeding allowable tolerances specified by welding codes/ standards on

- height of reinforcement

- underfill

- porosities

- undercut

- cracks

- cold laps

- Uniformity of bead ripples must be in accordance with welding standards

- Stringer or layered beads deposited in accordance with welding standards

- Finish weldment visually acceptable in accordance with welding standards for:

- spatters

- arc strikes

- slag

- uniformity of beads

CONTENTS:

- Essentials of welding

- International welding codes and standards

- Acceptable weld profiles

- Weld defects, causes and remedies

- Welding procedure specifications (WPS)

- Welding techniques and procedures

- Safe welding practices

CONDITIONS:

The student/trainee must be provided with the following:

1.	Equipment

- GMAW welding machine (AC/DC)

- Welding table or jig

- Portable grinder

- Welding booth

2.	Tools/ accessories

- Welding mask

- Steel brush

- Clear glass

- Chipping hammer

- Dark glass

3.	Supplies/ materials

- MIG wire

- Alloy steel plates

- Cutting grinding disk

      - Shielding gases

4.	Personal protective equipment

- Safety shoes

- Apron

- Leggings

- Safety goggles

- Gloves

5. Training materials

- GMAW welding manuals

- Welding procedures specifications (WPS)

- Welding standards

METHODOLOGIES:

- Lecture/demonstration

- Dualized

- Self-paced learning

ASSESSMENT METHODS:

- Written/oral

- Interview

- Direct observation

LO3.	Weld alloy Steel Plates in Vertical Position (3G)

ASSESSMENT CRITERIA:

  - Root penetration not exceeding allowable tolerances specified by welding codes/ standards on

- concavity

- convexity

- undercut

- excess penetration

- lack of fusion

- burn-through

- cracks

- Weld capping/ final pass not exceeding allowable tolerances specified by welding codes/ standards on

- height of reinforcement

- underfill

- porosities

- undercut

- cracks

- cold laps

- Uniformity of bead ripples must be in accordance with welding standards

- Stringer or layered beads deposited in accordance with welding standards

- Finish weldment visually acceptable in accordance with welding standards for:

- spatters

- arc strikes

- slag

- uniformity of beads

CONTENTS:

- Essentials of welding

- International welding codes and standards

- Acceptable weld profiles

- Weld defects, causes and remedies

- Welding procedure specifications (WPS)

- Welding techniques and procedures

- Safe welding practices

CONDITIONS:

The student/trainee must be provided with the following:

1.	Equipment

GMAW welding machine (AC/DC)

Welding table or jig

Portable grinder

Welding booth

2.	Tools/ accessories

Welding mask

Steel brush

Clear glass

Chipping hammer

Dark glass

3.	Supplies/ materials

MIG wire

steel plates

Cutting grinding disk

Shielding gases

4.	Personal protective equipment

Safety shoes

Apron

Leggings

Safety goggles

Gloves

5.	Training materials

GMAW welding manuals

Welding procedures specifications (WPS)

Welding standards

METHODOLOGIES:

- Lecture/demonstration

- Dualized

- Self-paced learning

ASSESSMENT METHODS:

- Written/oral

- Interview

- Direct observation

UNIT OF COMPETENCY	:	Weld ALLOY Steel PLATES USING GMAW

MODULE TITLE	:	Performing FILLET Welding on alloy Steel Plates

MODULE DESCRIPTOR	: 	This module covers the knowledge, skills and attitude in performing fillet welding on alloy steel plates in different positions such as 1G, 2G, & 3G and 1F, 2F, 3F & 4F.

NOMINAL DURATION	:	16 hours

SUMMARY OF LEARNING OUTCOMES:

Upon completion of this module the trainee/student must be able to:

LO1.	Weld alloy steel plates in flat position (1F)

LO2.   Weld alloy steel plates in horizontal position (2F)

LO3.   Weld alloy steel plates in vertical position (3F)

LO4.   Weld alloy steel plates in vertical position (4F)

LO1.	Weld ALLOY Steel Plates in Flat Position (1F)

ASSESSMENT CRITERIA:

  - Weld capping/ final pass not exceeding allowable tolerances specified by welding codes/ standards on

    - height of reinforcement

    - underfill

    - porosities

    - undercut

    - cracks

    - cold laps

- Uniformity of bead ripples must be in accordance with welding standards

3.   Stringer or layered beads deposited in accordance with welding standards

- Finish weldment visually acceptable in accordance with welding standards for:

    - spatters

    - arc strikes

    - slag

    - uniformity of beads

CONTENTS:

- Essentials of welding

- International welding codes and standards

- Acceptable weld profiles

- Weld defects, causes and remedies

- Welding procedure specifications (WPS)

- Welding techniques and procedures

- Safe welding practices

CONDITIONS:

The student/trainee must be provided with the following:

1.	Equipment

- GMAW welding machine (AC/DC)

- Welding table or jig

- Portable grinder

- Welding booth

2.	Tools/ accessories

- Welding mask

- Steel brush

- Clear glass

- Chipping hammer

- Dark glass

3. Supplies/ materials

- MIG wire

- Alloy steel plates

- Cutting grinding disk

      - Shielding gases

4.	Personal protective equipment

  - Safety shoes

  - Apron

  - Leggings

  - Safety goggles

  - Gloves

5.	Training materials

- GMAW welding manuals

- Welding procedures specifications (WPS)

- Welding standards

METHODOLOGIES:

- Lecture/demonstration

- Dualized

- Self-paced learning

ASSESSMENT METHODS:

- Written/oral

- Interview

- Direct observation

LO2.	Weld ALLOY Steel Plates in Horizontal Position (2F)

ASSESSMENT CRITERIA:

]

- Weld capping/ final pass not exceeding allowable tolerances specified by welding codes/ standards on

- height of reinforcement

- underfill

- porosities

- undercut

- cracks

- cold laps

- Uniformity of bead ripples must be in accordance with welding standards

- Stringer or layered beads deposited in accordance with welding standards

- Finish weldment visually acceptable in accordance with welding standards for:

- spatters

- arc strikes

- slag

- uniformity of beads

CONTENTS:

- Essentials of welding

- International welding codes and standards

- Acceptable weld profiles

- Weld defects, causes and remedies

- Welding procedure specifications (WPS)

- Welding techniques and procedures

- Safe welding practices

CONDITIONS:

The student/trainee must be provided with the following:

1.	Equipment

- GMAW welding machine (AC/DC)

- Welding table or jig

- Portable grinder

- Welding booth

2.	Tools/ accessories

- Welding mask

- Steel brush

- Clear glass

- Chipping hammer

- Dark glass

3.	Supplies/ materials

- MIG wire

- Alloy steel plates

- Cutting grinding disk

      - Shielding gases

4.	Personal protective equipment

- Safety shoes

- Apron

- Leggings

- Safety goggles

- Gloves

5.	Training materials

- GMAW welding manuals

- Welding procedures specifications (WPS)

- Welding standards

METHODOLOGIES:

- Lecture/demonstration

- Dualized

- Self-paced learning

ASSESSMENT METHODS:

- Written/oral

- Interview

- Direct observation

LO3.	Weld ALLOY Steel Plates in Vertical Position (3F)

ASSESSMENT CRITERIA:

- Weld capping/ final pass not exceeding allowable tolerances specified by welding codes/ standards on

- height of reinforcement

- underfill

- porosities

- undercut

- cracks

- cold laps

- Uniformity of bead ripples must be in accordance with welding standards

- Stringer or layered beads deposited in accordance with welding standards

- Finish weldment visually acceptable in accordance with welding standards for:

- spatters

- arc strikes

- slag

- uniformity of beads

CONTENTS:

- Essentials of welding

- International welding codes and standards

- Acceptable weld profiles

- Weld defects, causes and remedies

- Welding procedure specifications (WPS)

- Welding techniques and procedures

- Safe welding practices

CONDITIONS:

The student/trainee must be provided with the following:

1.	Equipment

- GMAW welding machine (AC/DC)

- Welding table or jig

- Portable grinder

- Welding booth

2.	Tools/ accessories

- Welding mask

- Steel brush

- Clear glass

- Chipping hammer

- Dark glass

3.	Supplies/ materials

- MIG wire

- Alloy steel plates

- Cutting grinding disk

      - Shielding gases

4.	Personal protective equipment

- Safety shoes

- Apron

- Leggings

- Safety goggles

- Gloves

5. 	Training materials

- GMAW welding manuals

- Welding procedures specifications (WPS)

- Welding standards

METHODOLOGIES:

- Lecture/demonstration

- Dualized

- Self-paced learning

ASSESSMENT METHODS:

- Written/oral

- Interview

- Direct observation

LO4.	Weld ALLOY Steel Plates in OVER HEAD Position (4F)

ASSESSMENT CRITERIA:

  - Weld capping/ final pass not exceeding allowable tolerances specified by welding codes/ standards on

- height of reinforcement

- underfill

- porosities

- undercut

- cracks

- cold laps

  - Uniformity of bead ripples must be in accordance with welding standards

  - Stringer or layered beads deposited in accordance with welding standards

  - Finish weldment visually acceptable in accordance with welding standards for:

- spatters

- arc strikes

- slag

- uniformity of beads

CONTENTS:

- Essentials of welding

- International welding codes and standards

- Acceptable weld profiles

- Weld defects, causes and remedies

- Welding procedure specifications (WPS)

- Welding techniques and procedures

- Safe welding practices

CONDITIONS:

The student/trainee must be provided with the following:

1.	Equipment

- GMAW welding machine (AC/DC)

- Welding table or jig

- Portable grinder

- Welding booth

2.	Tools/accessories

- Welding mask

- Steel brush

- Clear glass

- Chipping hammer

- Dark glass

3.	Supplies/ materials

- MIG wire

- Alloy steel plates

- Cutting grinding disk

      - Shielding gases

4.	Personal protective equipment

- Safety shoes

- Apron

- Leggings

- Safety goggles

- Gloves

5.	Training materials

- GMAW welding manuals

- Welding procedures specifications (WPS)

- Welding standards

METHODOLOGIES:

- Lecture/demonstration

- Dualized

- Self-paced learning

ASSESSMENT METHODS:

- Written/oral

- Interview

- Direct observation

UNIT OF COMPETENCY	:	Weld ALLOY Steel Pipe USING GMAW

MODULE TITLE	:	Performing Groove Welding on alloy Steel Pipes

MODULE DESCRIPTOR	: 	This module covers groove welding on alloy steel pipe in different positions such as 2G, 5G & 6G.

NOMINAL DURATION	:     40 hours

SUMMARY OF LEARNING OUTCOMES:

Upon completion of this module the trainee/student must be able to:

LO1.	Weld alloy steel pipes in horizontal position (2G)

LO2.	Weld alloy steel pipes in Fixed pipe horizontal position (5G)

LO3.	Weld alloy steel pipes in fixed pipe, inclined at 45( position (6G)

LO1.	Weld ALLOY Steel Pipe in Horizontal Position (2G)

ASSESSMENT CRITERIA:

- Root penetration not exceeding allowable tolerances specified by welding codes/ standards on

- concavity

- convexity

- undercut

- excess penetration

- lack of fusion

- burn-through

- cracks

- Weld capping/ final pass not exceeding allowable tolerances specified by welding codes/ standards on

- height of reinforcement

- underfill

- porosities

- undercut

- cracks

- cold laps

- Uniformity of bead ripples must be in accordance with welding standards

- Stringer or layered beads deposited in accordance with welding standards

- Finish weldment visually acceptable in accordance with welding standards for:

- spatters

- arc strikes

- slag

- uniformity of beads

CONTENTS:

- Essentials of welding

- International welding codes and standards

- Acceptable weld profiles

- Weld defects, causes and remedies

- Welding procedure specifications (WPS)

- Welding techniques and procedures

- Safe welding practices

CONDITIONS:

The student/trainee must be provided with the following:

1.	Equipment

- GMAW welding machine (AC/DC)

- Welding table or jig

- Portable grinder

- Welding booth

2.	Tools/ accessories

- Welding mask

- Steel brush

- Clear glass

- Chipping hammer

- Dark glass

3. Supplies/ materials

- MIG wire

- Alloy steel pipe

- Cutting grinding disk

      - Shielding gases

4. Personal protective equipment

- Safety shoes

- Apron

- Leggings

- safety goggles

- Gloves

5. Training materials

- GMAW welding manuals

- Welding procedures specifications (WPS)

- Welding standards

METHODOLOGIES:

- Lecture/demonstration

- Dualized

- Self-paced learning

ASSESSMENT METHODS:

- Written/oral

- Interview

- Direct observation

LO2.	Weld Alloy Steel Pipe in Fixed Pipe Horizontal Position (5G)

ASSESSMENT CRITERIA:

- Root penetration not exceeding allowable tolerances specified by welding codes/ standards on

  - concavity

  - convexity

  - undercut

  - excess penetration

  - lack of fusion

  - burn-through

  - cracks

- Weld capping/ final pass not exceeding allowable tolerances specified by welding codes/ standards on

  - height of reinforcement

  - underfill

  - porosities

  - undercut

  - cracks

  - cold laps

- Uniformity of bead ripples must be in accordance with welding standards

- Stringer or layered beads deposited in accordance with welding standards

- Finish weldment visually acceptable in accordance with welding standards for:

- spatters

- arc strikes

- slag

- uniformity of beads

CONTENTS:

- Essentials of welding

- International welding codes and standards

- Acceptable weld profiles

- Weld defects, causes and remedies

- Welding procedure specifications (WPS)

- Welding techniques and procedures

- Safe welding practices

CONDITIONS:

The student/trainee must be provided with the following:

1.	Equipment

- GMAW welding machine (AC/DC)

- Welding table or jig

- Portable grinder

- Welding booth

2.	Tools/ accessories

- Welding mask

- Steel brush

- Clear glass

- Chipping hammer

- Dark glass

3.	Supplies/ materials

- MIG wire

- Alloy steel pipe

- Cutting grinding disk

      - Shielding gases

4.	Personal protective equipment

- Safety shoes

- Apron

- Leggings

- Safety goggles

- Gloves

5.	Training materials

- GMAW welding manuals

- Welding procedures specifications (WPS)

- Welding standards

METHODOLOGIES:

- Lecture/demonstration

- Dualized

- Self-paced learning

ASSESSMENT METHODS:

- Written/oral

- Interview

- Direct observation

LO3.	Weld Alloy Steel Pipe in Fixed, Pipe Inclined at 45( PositionS (6G)

ASSESSMENT CRITERIA:

- Root penetration not exceeding allowable tolerances specified by welding codes/ standards on

- concavity

- convexity

- undercut

- excess penetration

- lack of fusion

- burn-through

- cracks

- Weld capping/ final pass not exceeding allowable tolerances specified by welding codes/ standards on

- height of reinforcement

- underfill

- porosities

- undercut

- cracks

- cold lap

- Uniformity of bead ripples must be in accordance with welding standards

- Stringer or layered beads deposited in accordance with welding standards

- Finish weldment visually acceptable in accordance with welding standards for:

- spatters

- arc strikes

- slag

- uniformity of beads

CONTENTS:

- Essentials of welding

- International welding codes and standards

- Acceptable weld profiles

- Weld defects, causes and remedies

- Welding procedure specifications (WPS)

- Welding techniques and procedures

- Safe welding practices

CONDITIONS:

The student/trainee must be provided with the following:

1.	Equipment

- GMAW welding machine (AC/DC)

- Welding table or jig

- Portable grinder

- Welding booth

2.	Tools/ accessories

- Welding mask

- Steel brush

- Clear glass

- Chipping hammer

- Dark glass

3.	Supplies/ materials

- MIG wire

- Alloy steel pipe

- Cutting grinding disk

- Shielding gases

4.	Personal protective equipment

- Safety shoes

- Apron

- Leggings

- Safety goggles

- Gloves

5.	Training materials

- GMAW welding manuals

- Welding procedures specifications (WPS)

- Welding standards

METHODOLOGIES:

- Lecture/demonstration

- Dualized

- Self-paced learning

ASSESSMENT METHODS:

- Written/oral

- Interview

- Direct observation

# What is Competency-Based Curriculum (CBC)

- A competency-based curriculum is a framework or guide for the subsequent detailed development of competencies, associated methodologies, training and assessment resources.

- The CBC specifies the outcomes which are consistent with the requirements of the workplace as agreed through the industry or community consultations.

- CBC can be developed immediately when competency standards exist.

- When competency standards do not exist, curriculum developers need to clearly define the learning outcomes to be attained. The standard of performance required must be appropriate to industry and occupational needs through the industry/enterprise or specified client group consultations.

These materials are available in both printed and electronic copies.

For more information please contact:

Technical Education and Skills Development Authority (TESDA)

Telephone Nos.: 893-8281, 817-4076 to 82 loc. 611 to 630, 631 and 635 or visit our website: www.tesda.gov.ph or the TESDA Regional or Provincial Office nearest you.